##### KXT-W型可曲挠橡胶接头

##### Model KXT-W Floating Flange Rubber Expansion Joints

##### Page28

#### 材料表

#### Table of Materilals

| 序号 Serial No | 部位 Prtion | 材料 Material |
| --- | --- | --- |
| 1 | 主体 Main body | 极性橡胶 Polarized rubber |
| 2 | 内衬 Lining | 尼龙帘布 Nylon cord fabric |
| 3 | 骨架 Frame | 硬钢丝 Hard steel wire |
| 4 | 法兰 Flange | 软钢 Mild steerl |

#### 技术条件

#### Technical Consition

| 公称通径 DN mm(寸) Nominal core diameter | 32-300(11/4"-12") | 350-500(14"-20") |
| --- | --- | --- |
| 工作压力 MPa(kg.f/cm2) Working pressure | 1.5(15) | 0.8(8) |
| 爆破压力 MPa(kg.f/cm2) Bursting pressure | 4.5(45) | 2.4(24) |
| 真空度 Vacuity Kpa(mm Hg) | 86.7(650) |
| 适用温度 Applicable temp. | -20℃-80℃(普通型) +80℃-135℃(特殊配方) |
| 适用介质 Applicable media | 空气、压缩空气、水、海水、热水、弱酸 Air.Compressed air.Water.Sea Water.Hot Water.Weak acid.Etc |
| 接头两端可任意偏转,便于自由调节轴向或横向位移.Both ends of the joint can be arbitray deflected for free adjustment of axial or lateral displacement. |

注：普通型产品中能在80℃以下，如需135℃以下需指明，更换橡胶配方。压力较高及冲击力较大时宜采用限位拉杆装置。

Note:ordinary type products can only be used under 80℃. if temperature is higher than 130℃, please show clearly, ingredient of the rubber will be changed. Restricting pull rod is necessary, when pressure is high and impulse is great.

#### 公称通径、长度、位移数值与法兰主要数据表

#### Table of Main Parameters of Nominal Core Diameter，Length，Displacement Value and Flange

| 公称能径 Nominal core diameter | 长度 Length l(mm) | 螺栓数 No.of bolt n | 螺栓孔直径 Diameter of bolt hole do(mm) | 螺栓孔中心圆 直径 Diameter of bolt hole center circlen D1 (mm) | 轴向位移 Axial displacenment(mm) | 横向位移 Lateral displace- ment (mm) | 偏转角度 Angle of deflection (α1+α2) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (mm) | (寸 in) |  |  |  |  | 伸长 Strech | 压缩 Compression |  |  |
| 32 | (11/4) | 150 | 130 | 4 | 15 | 89 | 12 | 20 | 14 | 150 |
| 40 | (11/2) | 150 | 130 | 4 | 15 | 98.5 | 12 | 20 | 14 | 150 |
| 50 | (2) | 150 | 130 | 4 | 19 | 121 | 12 | 20 | 14 | 150 |
| 65 | (21/2) | 150 | 130 | 4 | 19 | 139.5 | 12 | 20 | 14 | 150 |
| 80 | (3) | 150 | 130 | 4 | 19 | 153 | 12 | 20 | 14 | 150 |
| 100 | (4) | 150 | 130 | 8 | 19 | 190 | 12 | 20 | 14 | 150 |
| 125 | (5) | 150 | 130 | 8 | 22.5 | 216 | 12 | 20 | 14 | 150 |
| 150 | (6) | 150 | 130 | 8 | 22.5 | 242 | 12 | 20 | 14 | 150 |
| 200 | (8) | 150 | 130 | 8 | 22.5 | 298 | 12 | 20 | 14 | 150 |
| 250 | (10) | 150 | 130 | 12 | 22.5 | 362 | 16 | 25 | 22 | 150 |
| 300 | (12) | 150 | 130 | 12 | 22.5 | 432 | 16 | 25 | 22 | 150 |
| 350 | (14) | 200 | 12 | 28.5 | 476 | 16 | 25 | 22 | 150 |
| 400 | (16) | 200 | 16 | 28.5 | 540 | 16 | 25 | 22 | 150 |
| 450 | (18) | 200 | 16 | 32 | 578 | 16 | 25 | 22 | 150 |
| 500 | (20) | 200 | 20 | 32 | 634 | 16 | 25 | 22 | 150 |

注：其他标准或非标准法兰需另订协议，指明标准或提供图纸及有关数据，本厂可定制生产。法兰配备按需方提供，如JIS、DIN等，表中为ANSL150。

Note：For flanges ofother standards of non-standard, it is necessary to be agreed upon separately. please specify standard of furnish diagram and relative parameter, we will manufacture accordingly, ANSI150 are shown in the table.