##### BW-WJ型万向角向型波纹补偿器

##### BW-WJ universal angular corrugated compensator

##### Page42

BW-WJ型万向角向型波纹补偿器由一个（或二个及以上，即复式万向角向型）波纹管、销、 轴、铰链板、万向环和立板等结构件组成，能吸收任意一平面内的角位移并能承受波纹管压力推力的膨胀节，当需要大补偿量时，可采用两个或以上组合分段串联使 用，并对产品预压缩、拉伸或扭转安装。

BW-WJ universal angular corrugated compensator is made up of structures such as one (or more the two namely composite universal angular type) bellows, forelock, axis, hinge plate, universal loop and standing board etc. It can absorb angular displacement in any plane and bear the pressure or thrust of the bellows. When large compens-ation is required, two or more compensator can be assembled and utilized in series. Besides, the product can also be pre-pressed, pulled or reversed when installed.

#### 技术特性表： 疲劳寿命1500次
technical characteristics table: weary life of 1500 times.

| 公称通径 mm nominal diameter | 长度 mm length | 波纹管有效面积cm2 effective area of bellows | 角向补偿量（±°）/刚度N/mm angular compensating quantum士mm mm/rigidity N/mm |
| --- | --- | --- | --- |
|  |  |  | 1.0MPa | 1.6MPa | 2.5MPa |
| 40 | 300 | 21 | 4 | 6 | 4 | 13 | 4 | 16 |
| 50 | 300 | 41 | 4 | 7 | 4 | 15 | 4 | 18 |
| 65 | 350 | 61 | 6 | 8 | 6 | 10 | 6 | 12 |
| 80 | 350 | 82 | 6 | 14 | 8 | 18 | 8 | 25 |
| 100 | 350 | 125 | 8 | 15 | 8 | 25 | 8 | 50 |
| 125 | 400 | 180 | 16 | 18 | 15 | 28 | 15 | 60 |
| 150 | 400 | 255 | 16 | 20 | 15 | 30 | 15 | 72 |
| 200 | 450 | 480 | 18 | 24 | 16 | 32 | 16 | 80 |
| 250 | 450 | 730 | 20 | 50 | 18 | 56 | 18 | 95 |
| 300 | 500 | 1020 | 15 | 210 | 14 | 280 | 14 | 430 |
| 350 | 550 | 1280 | 15 | 220 | 14 | 300 | 14 | 450 |
| 400 | 550 | 1580 | 14 | 260 | 12 | 385 | 12 | 495 |
| 450 | 600 | 1980 | 12 | 320 | 10 | 710 | 10 | 1280 |
| 500 | 650 | 2450 | 10 | 515 | 8 | 890 | 8 | 1480 |
| 600 | 700 | 3450 | 10 | 1210 | 8 | 1620 | 8 | 1740 |
| 700 | 750 | 4740 | 10 | 1420 | 8 | 1820 | 6 | 3180 |
| 800 | 750 | 5960 | 8 | 1520 | 6 | 2410 | 4 | 3720 |
| 900 | 800 | 7560 | 4 | 1900 | 3 | 2750 | 3 | 4520 |
| 1000 | 850 | 9280 | 4 | 5100 | 3 | 8200 | 2 | 9200 |
| 1100 | 900 | 10816 | 3 | 11200 | 2 | 12600 | 2 | 15300 |
| 1200 | 900 | 13010 | 2 | 14800 | 2 | 15100 | 2 | 17600 |
| 1300 | 1000 | 14800 | 2 | 15100 | 2 | 18400 | 2 | 20800 |
| 1400 | 1000 | 16510 | 2 | 18500 | 2 | 23200 | 2 | 26800 |
| 1500 | 1100 | 18900 | 2 | 20600 | 2 | 26700 | 2 | 30800 |
| 1600 | 1200 | 21920 | 2 | 25100 | 2 | 30800 | 2 | 35200 |